## Slide 1: Finite Elements Modelling of Tritium Permeation
Tritium diffusion and convection in LiPb
Wilfrid Farabolini – Frédéric Dabbene

## Slide 2: A Fusion Power Reactor

## Slide 3: Schematic Fluids Circulation in the PPCS Reactor
JFW
J3
J5
Tritium extraction
from LiPb
He purification
QHe
LiPb
He
MHe
QPbLi
J1
J2
J4
Blower
Steam
generator
Secondary circuit
HCLL Blanket modules
LiPb
purification
Pump
air
purification
QPbLi
QHe
MLiPb
J1 = 610 g/day (4000 MW fusion power)
QHe = 4000 kg/s (Tin = 300°C, Tout = 500°C, P= 8.0 MPa

## Slide 4: Concept of the HCLL Blanket Modules
Demo Module
Breeding Unit

## Slide 5: Analytical Model – Tritium Mass Balance Equations 1/2
LiPb
He
J1
J2
J4
J3
J5
J1 / J5 =222650
day
/
g
610
J
1

J1 : Production rate
J2 : Extraction from LiPb
LiPb : extractor efficiency for LiPb
Cout : Tritium output concentration in LiPb (mol m-3),
GLiPb : LiPb flow rate (m3 s-1)
J3 : Permeation towards He coolant
Cave : Tritium average concentration in LiPb (mol m-3)
Kblanket: Blanket permeation factor (m3 s-1)
J4 : Extraction from He coolant
GHe : He flow rate to detritiation unit (m3 s-1)
( J5 max = 1 g/year=27 Ci/day , ITER standard )
J5 : Release to environment
LSG: Steam Generator leak flow (m3 s-1)
KSG: SG permeation factor (m3 s-1)

## Slide 6: Analytical Model – Tritium Mass Balance Equations 2/2
A, s : respectively wall surface (m2) and wall thickness (m).
Kssteel KsLiPb : Sievert constants (mol m-3 Pa-1/2), respectively in Eurofer and in LiPb
Dsteel Tritium diffusivity in Eurofer (m2 s-1)
PRFb is the Permeation Reduction Factor provided by permeation barrier (if any)
Stationary results (*) :
* Thanks to Italo Ricapito (ENEA consultant) who initiated these computations

## Slide 7: Computation of Kblanket for PPCS
For Tave=480 °C Ksteel Dsteel/KLipb = 2.7 10-8 m2 s-1
Kblanket = 1.09 /PRF m3 s-1

## Slide 8: Tritium flow towards He coolant (J3)
Kblanket = 1.09 / PRFb m3 s-1 (Tave = 480 °C, 180 modules)
LiPb = 0.8 (reasonable efficiency for packed column extractor)
GLiPb limitation due to LiPb velocity (MHD pressure drops and corrosion)
10 recycling/day
0.063 m3 s-1
72 recycling/day
0.454 m3 s-1

## Slide 9: Justification of the FEM Study
Previous analytical computations made the assumption that all the produced tritium is immediately available for permeation through the Eurofer walls.
Actually, T has to travel through the LiPb bulk before reaching the walls.
Considering that:
  T diffusivity in LiPb is about 10 times smaller than in Eurofer.
  LiPb layer thickness is 40 times larger than Cooling Plates wall thickness in present Breeding Unit design.
Ignoring these facts might lead to very pessimistic results (nearly all the produced T escapes into the He coolant, if no permeation barriers are used).
LiPb velocity
T produced in LiPb
T transport via diffusion
and convection through LiPb
T permeation through wall
He coolant flow

## Slide 10: CAST3M Model of the BU used for the study
p
r
600 mm
100 mm
1.08 mm
imposed input
T concentration
null T concentration
FW position
LiPb velocity with
various possible profiles
(Poiseuille, Flat, Hartmann)
computed T permeation flux
computed T
convection flux
margin for
numerical
stability
equivalent thickness
considering
He channels shape
r
T-source term
Q(r) = Qmax exp (– 4.5 r)
type of mesh used for
analytical-like computation
(homogeneous T concentration )
type of mesh used for
T diffusion computation
(stratified T concentration )
20 mm

## Slide 11: Cast3M results – homogeneous T concentration
v = 0.25 mm/s
18 recycling/day
83.2 % of permeation
v = 1.0 mm/s
72 recycling/day
39.9 % of permeation
v = 0.25 mm/s
v = 1.0 mm/s
Maximum T concentration
does not reached the outlet

## Slide 12: Diffusion with Poiseuille velocity profile
v = 0.25 mm/s
18 recycling/day
15.4 % of permeation
v = 1.0 mm/s
72 recycling/day
9.4 % of permeation

## Slide 13: Some velocity profiles induced by MHD
Hartmann wall
Side wall
from Magnetofluiddynamics in Channels and Containers, U. Müller, L. Bühler, Springer

## Slide 14: Diffusion with flat velocity profile
v = 0.25 mm/s
18 recycling/day
10.3 % of permeation
v = 1.0 mm/s
72 recycling/day
5.0 % of permeation

## Slide 15: Permeation vs. LiPb Velocity for various cases
10 recycling/day
0.063 m3 s-1
72 recycling/day
0.454 m3 s-1
(mm s-1)

forward and backward circulation

## Slide 16: Application of ITER duty factor (400 s / 1800 s)
v = 0.2 mm/s
v = 0.04 mm/s

## Slide 17: Conclusions
Taking into account T diffusion in the LiPb bulk drastically reduces the permeation rate as previously analytically computed.
Further works are to be completed to assess the LiPb flow (thermal convection with MHD, duct expansion/contraction, possible stagnation areas)
Further refinement can be introduced in the model (temperature chart for diffusivity, input T concentration, Stiffening Plates, 3D)
However, higher confidence in these results can only come from experimentation
Cast3M allows to fit TBM experiments in ITER in order to find Power Reactor equivalent working points